## Slide 1: Innerlayer Copper Balancing Phase 2
© HDP User Group International
Team Leader:
Facilitator:
Implementation
Asa Guest, IBM
Karl Sauter
October 17, 2024
Host: Virtual

## Slide 2: Background
Localized areas of Innerlayer Copper Imbalance can result in localized innerlayer core deformation.
  Increasing Zo variation across high speed channels
  Increases risk of Lamination voids, micro fracturing under large components
  Increased warpage & non-linear scaling
  Increases uncertainty/variation of layer z-axis location:
    Increasing backdrill stub variation
    Increased surface topology variations
Extent of Core deformation & Sensitivity to Inner Layer Copper Imbalance is an interaction between material selection and stackup.
Project Phase 1: Quantified sensitivity of void size and density stacking on core deformation, Surface topography for assembly, and recommended design approaches focused on Low Loss and Ultra Low-Loss laminates.
10/17/2024

## Slide 3: Phase 2 Motivation: Core Deformation and Insufficient Resin Fill
10/17/2024

## Slide 4: Phase 2 Motivation : Stackup and Material Selection
10/17/2024
Preventing core deformation requires filling voids on adjacent layers at same rate
When copper void volume is different between adjacent layers  prepreg thickness needs to be selected so that void fill rates are similar (most prominent with change in copper thickness)
Minimal deformation with either lower or higher flow when prepreg thickness match void volume ratio
Higher flow materials
Lower flow materials
High deformation with high flow
High deformation with low flow
Post Lamination

## Slide 5: Background - Continued
10/17/2024
Stackup-up (prepreg selection matters for thickness control):
For same material prepreg thickness mattered

## Slide 6: Project Deliverables Phase 2
10/17/2024
CAD translator utility available to members that will provide analysis of local copper distribution to identify risk areas for:
  Core deformation and backdrill stub variation
  Surface topography variations
  Local areas of glass stop
Potential feasibility to model extent of core deformation and/or surface topography variations.
Additional validation of the coplanarity and core deformation mitigation of using sub lam sequence and stack-up optimization.
  Phase 1 was a "hammer test" with respect to design
  Goal is to quantify extent that construction stack-up can overcome unbalanced designs

## Slide 7: Member Benefits
10/17/2024
OEM & Designers: Design guidelines for optimizing copper distributions;
  Minimize Impedance variations not captured in Zo coupons
  Minimize backdrill stub length variations under large BGAs
  Insight to influence of core deformation from copper distributions on dynamic warpage.
  Characterization of material properties and design on Surface Deformation
ODMs: Understand the impact of copper distributions on dynamic warpage and impact on boot issues w.r.t impedance (Zo) variations and/or stub control.
PCB Fabricators: Ability to highlight potential risk areas for designers and understand to what extent resin material flow properties modulate core deformation issues vs copper distribution.
Laminate Suppliers: Insight into the interaction between resin flow properties and design/ stackup parameters on core deformation.

## Slide 8: Member Benefits - Continued
The ability to automate the design analysis of designs for local copper balancing; reducing design costs, and time allowing more consistent electrical and topographical performance of the copper fill technique.
Additional validation of the coplanarity and core deformation mitigation of using sub lam sequence and stackup optimization. This will assure copper fill design rules are correct.
10/17/2024

## Slide 9: Status: Copper Balancing Analysis
10/17/2024
650um
0um
API utility from “Artwork Conversion Software, Inc.”
  Provide rolling grey scale average over a specified sliding window and window stepping for a single layer
    Allowing layer analysis w.r.t flow distances/properties of resin
    Ability to predict where deformation will start, locations of min/max deformation
  Provide ability to Add/Subtract multiple grey scale layers using layer weighting
Initial Wrapper created
to utilize API utility and
visualize results
Pixel size: 5x5mil
Total Copper
Visualization of 20% added thieving on signal layers

## Slide 10: Disclaimers
Blurring algorithms are used as rough approximations to capture
Cannot capture PP material under different lamination conditions

## Slide 11: Status: Copper Balancing Analysis
Example of Rolling Average over different distances
Pixel size at 5x5 mil
0.5 inch
1.25 inch
2.5 inch
Rolling average much better then simple averaging within a set grid w.r.t Maintaining a level of local detail otherwise hidden
Asymmetry of average thickness
Color bands around panel average
10/17/2024

## Slide 12: Interface Updates
Develop Interface for users to input stack up information/gerber data
  Assign Layer Details (Cu Weight, core/PP thickness)
Additional Averaging algorithms
Additional Image Options
  Pan/Zoom/Rotate
  Colorization (User Color Schemes Added)

## Slide 13: Status: Copper Balancing Analysis
Measured coplanarity variation of Q2
Shadow Moire
Total copper map of Q2 with rolling average
General patterns hold
Basic Shape of High/low areas
Location of Low/High Areas
Except when they don’t:
Panel 2, Mtrl A
Panel 1, Mtrl B
Panel 1, Mtrl A
650um
0um
10/17/2024

## Slide 14: Status: Copper Balancing Analysis
Measured coplanarity variation of Q4
Shadow Moire
Total copper map of Q4 with rolling average
General patterns hold
Basic Shape of High/low areas
Location of Low/High Areas
Panel 2, Mtrl A
Panel 1, Mtrl C
As expected: Total Cu map as an indicator of coplanarity will be best when Local Thickness variations are dominate factor in Coplanarity
650um
0um
10/17/2024

## Slide 15: Stackup Modulation of Core Deformation On Hold until initial modeling more complete
10/17/2024
Use same TV from Phase 1 (22 layers, w/ six 2-oz layers)
Ensure any builds use same laminate / PCB fabricator combinations
  Build A: Increase prepreg thickness next to 2-oz layers by 100-150%
    Change the resin volume to match or exceed fill rate of adjacent 1-oz layers
    Goal to minimize or even flip direction of core deformation toward center
  Build option B: Fabricate the center 2-oz layers as sublam to decouple 1-oz vs 2-oz deformation.
Build option C: Hybrid construction using higher flow materials at center 2-oz
Analysis of surface topography and core deformation same as Phase 1
Builds only require fabrication through panel plate

## Slide 16: Interface
Gerber to Tiff In App
In App Image View
Operations for stack up information from gerber layers
Preset/User defined color mappings

## Slide 17: Interface
Layer specific modifications
Sub lamination Analysis
Additional user defined settings

## Slide 18: MetAve algorithm (Box Filter)
Command line executable
  Image operations become a file management issue
  Algorithm is
  Assumes boundaries are 0
Inputs
  Input Layers
  Layer Weighting
  Averaging window
Weighted Result
Rolling average of target
N
N
Ncell(x, y)
r = 2

## Slide 19: Gaussian Algorithm
Accessed through the Scipy (pythons scientific computing library)
Algorithm is
Adjustable parameters
  Etc.
May approximate physics closer than box blur

## Slide 20: Additional Algorithms To be Added
Median Filter
Bilateral Filter
Open to adding others

## Slide 21: Asymmetry from Symmetric Design & Stackup
Asymmetric location of resin flow and core deformation likely critical to panel-panel variations in Co-Planarity and backdrill layer location.
Hypothesized to be related to book placement. But, outside of scope/focus of Phase 2
Why more resin here?
Stackup is symmetrical
10/17/2024

## Slide 22: Project Flow Chart -
Fabrication
Evaluation
X-Section – Core Deformation measurements (1-2 panels/mtrl)
Design
(Cmplt)
Supplier 1 | Lower Flow Ultra Low Loss Laminate system Thick Prepreg @ 2oz lyrs 5 panels
Supplier 2 | 
Surface Topography (all panel/mtrl)
Data Analysis
Final Report
Supplier A | Lower Flow Ultra Low Loss Laminate system Hybrid 5 panels
Supplier B | 
Supplier C | Lower Flow Ultra Low Loss Laminate system Phase1 stackup w/ sublam 5 panels
Supplier D | 
Artwork Dev
Manual Testing
/ Verification
Wrapper Dev
Stackup Modulation of Core Deformation
Analysis Tool Dev

## Slide 23: Resources and Schedule
Task | Resource | Planned | Actual
Complete DOE Matrix | All |  | Complete
TV Design ECAD | Intel |  | Complete
PCB Laminate Materials | EMC, Iteq, AGC, TUC | TBD | 
TV Fabrication | TTM, WUS, VGT, SCC, Founder, SME, ACCL |  | 
Surface Characterization | Akrometrix |  | 
Microsection Analysis | Intel |  | 
Final Report | All |  | 
MetAve software dev | Artwork Conversion Inc | 16 weeks | Complete
MetAve Testing / analysis | Intel | 20 weeks | WIP
Wrapper Dev | Intel | 16 weeks | 

## Slide 24: Team List
IBM - leader
AGC
Akrometrix
Panasonic
Oracle
Nokia
Juniper
WUS
Resonac
VGT
TTM
EMC
ITEQ
TUC
Co-Tech Development
Sanmina
Intel

## Slide 25
Thank You
For questions or comments on this presentation,
please email: karls@hdpug.org